### SECTION 09 50 00

### SoundScapes® Blades Linear Acoustical Panels – Colors

### PART 1 - GENERAL

### 1.1 RELATED DOCUMENTS

Drawings and general conditions of Contract, including General and Supplementary Conditions and Divisions-1 Specification sections apply to work of this section.

### 1.2 SUMMARY

- Section Includes:

  - Linear acoustical ceiling and wall panels

  - Exposed grid suspension system

  - Wire hangers, fasteners, main runners, cross tees, wall angle moldings and accessories

- Related Sections:

  - Section 09 51 00 – Acoustical Ceilings

  - Section 09 53 00 – Acoustical Ceiling Suspension Assemblies

  - Section 09 54 33 – Decorative Panel Ceilings

  - Section 09 20 00 – Gypsum Board

  - Division 23 – HVAC Air Distribution Mechanical Work Division

  - Division 26 – Electrical Work

- Alternates

  - Prior Approval: Unless otherwise provided for in the Contract documents, proposed product substitutions may be submitted no later than TEN (10) working days prior to the date established for receipt of bids. Acceptability of a proposed substitution is contingent upon the Architect's review of the proposal for acceptability and approved products will be set forth by the Addenda. If included in a Bid are substitute products which have not been approved by Addenda, the specified products shall be provided without additional compensation.

  - Submittals which do not provide adequate data for the product evaluation will not be considered. The proposed substitution must meet all requirements of this section, including but not necessarily limited to, the following: Single source materials suppliers (if specified in Section 1.5); Underwriters' Laboratories Classified Acoustical performance; Panel design, size, composition, color, and finish; Suspension system component profiles and sizes; Compliance with the referenced standards.

### 1.3 REFERENCES

- American Society for Testing and Materials (ASTM):

  - ASTM A 1008 Standard Specification for Steel, Sheet, Cold Rolled, Carbon, Structural, High-Strength Low-Alloy and High-Strength Low-Alloy with Improved Formability

  - ASTM A 641 Standard Specification for Zinc-Coated (Galvanized) Carbon Steel Wire

  - ASTM A 653 Standard Specification for Steel Sheet, Zinc-Coated (Galvanized) by the Hot-Dip Process

  - ASTM C 423 Sound Absorption and Sound Absorption Coefficients by the Reverberation Room Method

  - ASTM C 635 Standard Specification for Metal Suspension Systems for Acoustical Tile and Lay-in Panel Ceilings

  - ASTM C 636 Recommended Practice for Installation of Metal Ceiling Suspension Systems for Acoustical Tile and Lay-in Panels

  - ASTM E 84 Standard Test Method for Surface Burning Characteristics of Building Materials

  - ASTM D 3273 Standard Test Method for Resistance to Growth of Mold on the Surface of Interior Coatings in an Environmental Chamber

  - ASTM E 580 Standard Practice for Installation of Ceiling Suspension Systems for Acoustical Tile and Lay-in Panels in Areas Subject to Earthquake Ground Motions

- NFPA 286 Standard Methods of Fire Tests for Evaluating Contribution of Wall and Ceiling Interior Finish to Room Fire Growth

- ASHRAE Standard 62.1-2004, “Ventilation for Acceptable Indoor Air Quality”

- ICC ESR 1308 International Code Council Evaluation Report Independent Evaluation of Armstrong Suspension Components for Seismic Installations

- International Building Code

- ASCE 7 American Society of Civil Engineers, Minimum Design Loads for Buildings and Other Structures

- International Code Council-Evaluation Services - AC 156 Acceptance Criteria for Seismic Qualification Testing of Non-structural Components

- LEED - Leadership in Energy and Environmental Design is a set of rating systems for the design, construction, operation, and maintenance of green buildings

### 1.4 SUBMITTALS

- Product Data: Submit manufacturer's technical data for each type of acoustical ceiling unit and suspension system required.

- Samples: Minimum 6” x 6” submittal sample of specified blade color; 8 inch long sample of suspension system, including main runner and cross tee.

- Shop Drawings: Layout and details of acoustical ceilings show locations of items, which are to be coordinated with, or supported by the ceilings.

- Certifications: Manufacturer's certifications that products comply with specified requirements, including laboratory reports showing compliance with specified tests and standards.

### 1.5 QUALITY ASSURANCE

- Single-Source Responsibility: Provide acoustical panel units and grid components by a single manufacturer.

- Fire Performance Characteristics: Identify acoustical ceiling components with appropriate markings of applicable testing and inspecting organization.

  - Surface Burning Characteristics: Class A as follows, tested per ASTM E84 and CAN/ULC S102:

    - Flame Spread: 25 or less

    - Smoke Developed: 50 or less

- Handle acoustical blades carefully to avoid scratching or denting units in any way.

### 1.6 DELIVERY, STORAGE, AND HANDLING

- Deliver acoustical ceiling units to project site in original, unopened packages and store them in a fully enclosed space where they will be protected against damage from moisture, direct sunlight, surface contamination, and other causes.

- Before installing acoustical ceiling units, permit them to reach room temperature and a stabilized moisture content.

- Handle acoustical ceiling units carefully to avoid chipping edges or damaged units in any way.

### 1.7 PROJECT CONDITIONS

- Space Enclosure:

All ceiling products and suspension systems must be installed and maintained in accordance with Armstrong written installation instructions for that product in effect at the time of installation and best industry practice. Prior to installation, the ceiling product must be kept clean and dry, in an environment that is between 32°F (0°C) and 120°F (49°C) and not subject to Abnormal Conditions. Abnormal conditions include exposure to chemical fumes, vibrations, moisture from conditions such as building leaks or condensation, excessive humidity, or excessive dirt or dust buildup.

HumiGuard Plus Ceilings: Installation of the products shall be carried out where the temperature is between 32°F (0° C) and 120°F (49° C). It is not necessary for the area to be enclosed or for HVAC systems to be functioning. All wet work (plastering, concrete, etc.) must be complete and dry. The ceilings must be maintained to avoid excessive dirt or dust buildup that would provide a medium for microbial growth on ceiling panels. Microbial protection does not extend beyond the treated surface as received from the factory and does not protect other materials that contact the treated surface such as supported insulation materials.

### 1.8 WARRANTY

- Blades: Submit a written warranty executed by the manufacturer, agreeing to repair or replace acoustical panels that fail within the warranty period. Failures include, but are not limited to:

  - Blade Panels: Sagging and warping as a result of defects in materials or factory workmanship.

  - Grid System: Rusting and manufacturer's defects

- Warranty Period:

  - Blades: One (1) year from date of substantial completion

  - Suspension System: Ten (10) years from date of substantial completion

- The Warranty shall not deprive the Owner of other rights the Owner may have under other provisions of the Contract Documents and will be in addition to and run concurrent with other warranties made by the Contractor under the requirements of the Contract Documents.

### 1.9 MAINTENANCE

- Extra Materials: Deliver extra materials to Owner. Furnish extra materials described below that match products installed. Packaged with protective covering for storage and identified with appropriate labels.

  - Acoustical Ceiling Units: Furnish quality of full-size units equal to 5.0 percent of amount installed.

  - Exposed Suspension System Components: Furnish quantity of each exposed suspension component equal to 2.0 percent of amount installed.

### Part 2-PRODUCTS

### 2.1 MANUFACTURERS

### (Select the appropriate Blade Design, Size and Color before finalizing the specification. Remove unused Linear Ceiling units)

### 2.2. LINEAR CEILING UNITS

- Basis of Design SoundScapes Blades

  - Armstrong World Industries Inc.

- Suspension System

  - Armstrong World Industries Inc.

### 2.2.1 SoundScapes Blades:

- Surface Texture: Fine

- Composition: Fiberglass

- Color: White (DWH), Black (DBL), Riverstone (DRV), Stone (DSE), Oat (DOT), Light Grey (DLG), Sandstone (DSS), Boxwood (DBW), Fern (DFN), Ivy (DIV), Ocean (DOC), Twilight (DTT), Rainstorm (DRS), Mist (DMT), Topaz (DTZ)

- Size & Design:

5 x 46 x 1-3/4” Rectangle (item 8250F03RH05), 
5 x 94 x 1-3/4” Rectangle (item 8250F03RH06), 
10 x 46 x 1-3/4” Rectangle (item 8250F03RH01), 
10 x 94 x 1-3/4” Rectangle (item 8250F03RH02), 
16 x 46 x 1-3/4” Rectangle (item 8250F03RH07), 
16 x 94 x 1-3/4” Rectangle (item 8250F03RH08), 
22 x 46 x 1-3/4” Rectangle (item 8250F03RH03), 
22 x 94 x 1-3/4” Rectangle (item 8250F03RH04), 
28 x 46 x 1-3/4” Rectangle (item 8250F03RH09), 
28 x 94 x 1-3/4” Rectangle (item 8250F03RH10), 
7-1/2 x 46 x 1-3/4” Hill (item 8250F03CH01), 
10-1/2 x 46 x 1-3/4” Valley (item 8250F03CH02), 
19-1/2 x 46 x 1-3/4” Hill (item 8250F03CH03), 
22-1/2 x 46 x 1-3/4” Valley (item 8250F03CH04), 
10-1/2 x 94 x 1-3/4” Wave (item 8250F03WH01), 
22-1/2 x 94 x 1-3/4” Wave (item 8250F03WH02), 
10 x 46 x 1-3/4” Wave (item 8250F03WH03),
22 x 46 x 1-3/4” Wave (item 8250F03WH04), 
10 x 94 x 1-3/4” Double Wave (item 8250F03WH05), 
22 x 94 x 1-3/4” Double Wave (item 8250F03WH06)

- Edge Profile: Square

- Recycled Content: 43%

- Acoustics: Sound absorption up to 1.80 NRC dependent on blade depth and spacing

| Panel Depth | 6” O.C. | 12” O.C. | 18” O.C. | 24” O.C. |
| --- | --- | --- | --- | --- |
| 5” | 0.80 | 0.50 | 0.40 | 0.30 |
| 7-1/2” | 1.00 | 0.65 | 0.50 | 0.40 |
| 10” | 1.15 | 0.80 | 0.60 | 0.50 |
| 10-1/2” | 1.15 | 0.80 | 0.60 | 0.50 |
| 16” | 1.35 | 1.00 | 0.75 | 0.55 |
| 19-1/2” | 1.40 | 1.00 | 0.75 | 0.60 |
| 22” | 1.45 | 1.00 | 0.75 | 0.65 |
| 22-1/2” | 1.45 | 1.00 | 0.80 | 0.65 |
| 28” | 1.80 | 1.35 | 1.10 | 0.95 |

- Flame Spread: ASTM E 1264; Class A (UL)

- Dimensional Stability: HumiGuard Plus; Anti-Microbial, inherent

- Acceptable Product: SoundScapes Blades, (item XXXX) as manufactured by Armstrong World Industries

2.2.2 Individual Suspension:

- Aircraft Cable: Acceptable product as manufactured by Armstrong World Industries

  - Item 6655 - 4-Point Hanging Kit (4 per bag)

  - Item 625530 - Extended Hanging Aircraft Cables (30' length, 4 per bag). For use with Item 6655 when longer cables are needed.

2.3.1	METAL SUSPENSION SYSTEMS

- Direct-to-Grid Suspension Acceptable Product: Listed Below as manufactured by Armstrong World Industries, Inc. Items are available in custom colors; contact ASQuote@armstrongceilings.com.

  - Prelude XL in coordinating finishes manufactured by Armstrong World Industries:

7301 _ _ _ 12' HD Main Beam

XL7342 _ _ _ 4' Cross Tee

XL7328 _ _ _ 2' Cross Tee

7800 _ _ _ 12’ Angle Molding

  - 360° painted Black (BL) or White (WH) as manufactured by Armstrong World Industries:

730136 12’ HD Main Beam

XL734036 4’ Cross Tee

XL732036 2’ Cross Tee

780036 12’ Angle Molding

  - 360° painted made to order colors (RAL) as manufactured by Armstrong World Industries:

56418 12’ HD Main Beam

56421 4’ Cross Tee

56419 2’ Cross Tee

7800 12’ Angle Molding

- Direct-Attach Acceptable Product: AXM34STR3 _ _ 10' Straight Wall Molding (360º Paint Recommended)

- Wire for Hangers and Ties: ASTM A 641, Class 1 zinc coating, soft annealed, with a yield stress load of at least time three design load, but not less than 12 gauge.

- Accessories (based on selection)

AX4STR3_ _ 10’ Axiom Classics 4” Straight Trim (360º Paint Recommended)

ARBRKT Adjustable Hanger Bracket

6459BL Black Rigid Attachment Clip

STAC Single Tee Adapter Clip

- Seismic Accessories Required (based on “Seismic Design Category”)

### PART 3 - EXECUTION

### 3.1 EXAMINATION

- Do not proceed with installation until all wet work such as concrete, terrazzo, plastering and painting has been completed and thoroughly dried out, unless expressly permitted by manufacturer's printed recommendations. (Exception: HumiGuard Max Ceilings)

### 3.2 PREPARATION

- Coordination: Furnish layouts for preset inserts, clips, and other ceiling anchors whose installation is specified in other sections.

  - Furnish concrete inserts and similar devices to other trades for installation well in advance of time needed for coordination of other work.

### 3.3 INSTALLATION

### Install SoundScapes Blades per Armstrong World Industries installation instructions.

### For areas having seismic requirements, consult with the Authority Having Jurisdiction or Building Code to determine the local requirements and following the manufacturers seismic guidelines found in the manufacturers Installation instructions.

### Install suspension system per ASTM C636 unless otherwise noted in the manufactures Installation Instructions.

### 3.4 ADJUSTING AND CLEANING

- Replace damaged and broken blades.

- Clean exposed surfaces of blades, including trim, and suspension members comply with manufacturer's instructions for cleaning and touch up of minor finish damage.

- Remove and replace work that cannot be successfully cleaned and repaired to permanently eliminate evidence of damage.

### END OF SECTION